## 1. What Can Be Bought or Built Today

Within the screened set, the most “buildable today” options for manufacturing wastes (swarf, grinding sludge/slurry, leachates arising from manufacturing scrap processing) are conventional hydrometallurgical precipitation and solvent-extraction-style flowsheets, plus adsorbent polishing of hydromet wastewaters; the evidence base in the excerpts is largely bench/lab, with one TEA/LCA-style industrial model for swarf processing. Acid-free dissolution with copper(II) nitrate is presented as an industrially modeled route for NdFeB magnet swarf (powders/filings from cutting and grinding), with downstream precipitation/filtration and oxide production steps (dissolution, filtration, ammonium hydroxide precipitation, oxalic acid precipitation, and roasting to mixed REOs).

For solvent extraction, a D2EHPA-in-kerosene route is demonstrated at bench scale with counter-current staging and quantified co-extraction behavior (Fe/B/Co), and a coupled approach using solvent extraction plus extraction chromatography is described to split REEs into separate fractions under sulfuric-acid elution conditions.

For “shop-floor” solids handling before hydromet (i.e., reducing iron interference before leaching), one recent process uses flash reduction plus two-step wet magnetic separation on scraps produced during cutting, grinding, and polishing, explicitly sourced from a magnet manufacturer (Ganzhou YouLi Technology). This is a pre-concentration route that increases REOs in a REO-rich phase and enriches an Fe-rich phase, with the stated benefit of minimizing Fe interference in subsequent leaching and avoiding substantial leaching waste residue rich in rare earth phases.

On the “removal from wastewater” end (rather than bulk recovery from solids), a nitrogen-rich hydrogel adsorbent (PEI-ALG@KLN) is presented for “waste NdFeB magnet hydrometallurgical wastewater,” with reported Nd/Dy recovery and Fe rejection, suggesting a plausible polishing/secondary recovery unit operation after hydromet steps where an aqueous stream exists.

Named commercial entities appearing in the provided excerpts are primarily suppliers of reagents or feedstock rather than turnkey wastewater vendors: D2EHPA (97%) is stated as supplied by Sigma Aldrich, and manufacturer-provided scrap is attributed to Ganzhou YouLi Technology (Ganzhou, China).

## 2. Best Credible Benchmarks

The table below summarizes the best extractable, quantitative benchmarks in the provided excerpts, separated by whether the process targets bulk recovery from solids/leachates or adsorption from a wastewater stream. All values are reported as stated, with the evidence level indicated.

| Technology class | Waste stream type | Best Nd metric | Best Dy metric | Best Pr metric | Evidence level |
| --- | --- | --- | --- | --- | --- |
| Hydromet (acid-free dissolution + precipitation to mixed REOs) | Magnet swarf from cutting/grinding | Overall REE extraction/recovery efficiency 96%–99% (baseline 97%) | Dy treated as part of mixed REO output; scenarios assume 0.48% Dy in swarf (baseline) and vary Dy to 0% and 6% alongside 96%–99% leaching assumptions | Pr treated as part of mixed REO output; baseline assumes 3.33% Pr in swarf | TEA/LCA estimate based on lab data and equipment sizing |
| Hydromet + solvent extraction (D2EHPA SX) | PLS (leachate) from NdFeB waste | 99.9% Nd extraction with three counter-current stages; >80% Nd stripped using 1.25 M H2SO4 at 25 °C (A/O 0.5) | >99.7% Dy extraction; >99% Dy extraction at pH 1.9 | 92% Pr extraction | Lab-scale (250 mL beaker SX/stripping) |
| Ion exchange/resin (extraction chromatography with D2EHPA-impregnated column) | PLS fed to column (Nd 462 mg/L; Pr 38 mg/L) | Nd+Pr fraction purity >98%; Nd fraction target below 0.01% Sm | Dy recovered last; Dy elution requires >0.9 M H2SO4 | >50% Pr recovery in a third fraction with purity >75% (real PLS) | Lab-scale (50 µL injections; 1 mL/min eluate flowrate) |
| Hydromet (AMSS roasting + HCl leach + oxalate precipitation + calcination) | Swarf/slurry with coolant (AMSS includes 52.5% cooling reagent) | 99% Nd dissolved in 0.5 N HCl; 99% Nd recovery; 18 g oxalic acid per L solution to precipitate 99% Nd; final product purity “over 99%” | Not found in provided excerpts (not reported quantitatively) | Not found in provided excerpts (not reported quantitatively) | Lab-scale (older, 2018) |
| Biological/biosorption (PEI-ALG@KLN hydrogel adsorbent) | “Waste NdFeB magnet hydrometallurgical wastewater” | Nd adsorption capacity 125 mg/g; Nd recovery rate >93%; capacity remains >85% after five adsorption–desorption cycles | Dy recovery rate >93% (reported jointly with Nd) | Not found in provided excerpts (not reported quantitatively) | Lab-scale |
| Other (flash reduction + magnetic separation) | Scraps from cutting/grinding/polishing | Not found in provided excerpts (element-specific Nd not reported) | Not found in provided excerpts | Not found in provided excerpts | Lab-scale (100 g processed; ~5 s flash reduction residence time) |

Across the hydromet/SX pathways, the strongest Nd and Dy extraction numbers in the provided excerpts are from the staged D2EHPA solvent extraction experiments (99.9% Nd extraction; >99.7% Dy extraction). In contrast, the adsorption approach reports >93% recovery (Nd and Dy) and provides an Nd adsorption capacity (125 mg/g), but does not (in the provided excerpts) report wastewater discharge limits, residual concentrations, or full-stream mass balances that would be required to benchmark it against industrial effluent compliance needs.

For costs and energy, only the TEA/LCA-style swarf process provides explicit, extractable cost and energy assumptions in the provided excerpts: total cost of $1,092,585–$1,525,596/year (also expressed as ~$11 per kg of swarf processed or ~$29–$36 per kg of mixed REO produced), filtration energy assumed as 5.5 kWh/ton of dry material, and roasting energy reported as 16 kWh/kg of REO (4 kW muffle furnace; up to 4 hours per 1 kg REO).

## 3. Dominant Hidden Costs and Burdens

The dominant “hidden costs” visible in the excerpts are not line-item OPEX tables (which are generally absent from the lab-scale papers), but rather the pretreatment requirements, interference management, and secondary solids/wastewater streams implied by the chemistry and separations used.

A recurring burden is iron management. In the acid-free dissolution route, dissolution produces an REE-containing solution alongside copper and iron precipitates that must be separated by filtration, and an additional wastewater-treatment step is described to remove iron using calcium chloride and calcium hydroxide (prepared from calcium oxide). In the D2EHPA SX route, co-extraction is quantified (7% Fe, 4% B, 2% Co across three counter-current stages), and downstream handling is implied in the need for scrubbing (oxalic acid scrubbing enabling >86% Fe and >88% B scrubbing). In the same source family, the raffinate iron-removal step is described as potentially slow, with precipitation rates requiring control to maintain filterability, which signals a time-and-solids-handling penalty even when the solvent-extraction step itself performs well.

Another recurring burden is coolant/organic content in manufacturing slurries. The AMSS (acoustic magnet swarf slurry) is described as containing 52.5% cooling reagent, and oxidation roasting is described as serving to remove cooling reagent and decrease iron dissolution, implying a significant thermal pretreatment and organic handling step to make leaching workable. Consistent with this, the AMSS route includes multiple high-temperature steps (e.g., oxidation roasting at 600 °C for 6 hours; calcination at 900 °C for 0.5 hour) and elevated-temperature leaching (e.g., 95 °C for 4 hours), which collectively imply substantial equipment and energy burdens even when direct Nd recovery is high in lab tests.

Pre-concentration by flash reduction plus magnetic separation is positioned as a way to reduce Fe interference and to avoid substantial leaching waste residue rich in rare earth phases, which is a different kind of “hidden cost” lever: shifting burden upstream into thermal reduction and physical separation to reduce downstream residue and leach complexity.

Finally, reagent circularity and loss can be a major burden. In the acid-free copper-nitrate dissolution TEA/LCA, copper nitrate is identified as a primary source of non-carcinogenics and ecotoxicity impacts, and copper nitrate recycling efficiency is stated as ~70%, implying ongoing reagent makeup and associated burden even under a “recycling” design.

## 4. Biological Win and Fail Conditions

The provided excerpts suggest two plausible incumbent benchmarks for a biological or bio-derived sorbent approach: (i) high extraction performance from hydromet/SX routes, and (ii) quantified Fe/REE discrimination. In staged D2EHPA solvent extraction, the benchmark extraction values reported are 99.9% Nd extraction and >99.7% Dy extraction under the stated counter-current staging, with quantified co-extraction (7% Fe, 4% B, 2% Co). In the PEI-ALG@KLN adsorption work, the benchmark values reported are >93% recovery for Nd and Dy, Nd capacity 125 mg/g, and Fe recovery only 5.04%, with >85% capacity retention after five adsorption–desorption cycles.

A credible set of biological win conditions (as hypotheses anchored to the extracted numbers) is therefore:

- The bio-based route should demonstrate Nd and Dy recovery that is at least comparable to the reported >93% recovery values, while maintaining strong Fe rejection comparable to Fe recovery of 5.04% in the adsorbent example.

- The bio-based route should show stability over multiple reuse cycles at least comparable to “capacity remains more than 85% after five adsorption–desorption cycles,” because regeneration durability directly affects consumables and waste burdens for sorbent systems.

- If competing directly with solvent extraction for leachates, the bio-based route must be evaluated head-to-head against the very high extraction benchmarks reported for SX (99.9% Nd; >99.7% Dy), which likely necessitates either multi-stage contacting or a process design that can deliver comparable overall recovery at realistic flow and solids loads.

Corresponding biological fail conditions (again, hypotheses grounded in incumbent numbers) include:

- Strong performance collapse in the presence of iron-bearing matrices, because iron interference is a repeatedly surfaced operational issue across hydromet and SX routes (filtration of Fe/Cu precipitates, iron precipitation control for filterability, co-extraction that demands scrubbing).

- Inability to operate on coolant-laden or organic-contaminated streams without upstream destruction or removal, because manufacturing slurries can contain large coolant fractions (e.g., 52.5% cooling reagent in AMSS) and roasting is used explicitly to remove these organics before leaching in one manufacturing-slurry flowsheet.

## 5. Plant Baseline

The excerpts provide clear descriptions of where manufacturing wastes arise (e.g., magnet swarf as powders and filings from cutting and grinding; scraps produced during cutting, grinding, and polishing; grinding sludge from the sintered-magnet production process). They also show why these wastes are operationally challenging (e.g., AMSS described as 52.5% cooling reagent).

However, the provided excerpts do not contain an explicit, quantitative description of the prevailing in-plant “do-nothing” handling route (e.g., direct disposal routes, on-site neutralization-only, off-site hazardous waste classification, or internal returns to melt) for these manufacturing waste streams. A practical baseline-assessment approach consistent with the burdens described in the technical excerpts is to document: (i) where iron is removed (e.g., CaCl2 + Ca(OH)2 iron removal is described as a wastewater-treatment step in one TEA/LCA), (ii) whether coolant-rich slurries are thermally treated (oxidation roasting described as removing cooling reagent), and (iii) whether any plant already deploys physical pre-concentration to reduce leach residue burdens (flash reduction + magnetic separation described as avoiding substantial leaching waste residue).

## 6. Top Data Gaps

The gaps below are ranked by decision impact and time-to-resolve, and each includes a concrete retrieval plan. The list is constrained to what the excerpts explicitly do and do not report.

- Element-specific Dy and Pr performance on true manufacturing wastewaters (not just leachates). Dy and Pr metrics are often absent in the manufacturing slurry and sludge routes, while Nd is reported more frequently (e.g., AMSS Nd dissolution/recovery is quantified, but Dy/Pr are not). Retrieval plan: measure Nd/Pr/Dy concentrations (ICP-OES/ICP-MS) in influent/effluent streams for pilot trials on manufacturing coolants/rinse waters; look for plant wastewater monitoring reports and hydromet bleed-stream analyses.

- Residual concentrations and discharge metrics for any technology applied to manufacturing wastewaters (mg/L after treatment). The adsorbent work reports recovery rates and capacity but not discharge endpoints in the excerpts. Retrieval plan: run batch and column tests reporting effluent concentration vs bed volumes; internal EHS compliance records typically capture discharge concentrations by outfall and permit parameter.

- Pretreatment requirements for adsorbent use, including pH control, solids filtration, and regeneration chemistry. The adsorbent excerpts mention adsorption–desorption cycling but do not specify regeneration reagents. Retrieval plan: obtain full text methods and supporting information; request vendor-style regeneration protocol; verify via mass balance on eluate/reagent consumption per cycle.

- Full reagent consumption rates for hydromet leaching and precipitation steps. One route reports oxalic acid demand as “18 grams” per “litre of solution,” but broader reagent consumption (acid/base neutralization demand, scrubbing reagent) is not consistently enumerated in excerpts. Retrieval plan: from process design packages, compile reagent make-up and bleed; lab can measure titration curves (acid/base demand) and precipitation yields vs dosage.

- Secondary waste quantities and characterization (filter cake mass, hazardous classification, Cu/Fe sludge). Filtration of Cu/Fe precipitates and iron precipitation control are described, but not the resulting sludge quantities. Retrieval plan: measure solids generation (kg dry solids per m³ treated) and TCLP/metals; look for waste manifests and sludge dewatering logs from similar hydroxide precipitation systems.

- Economic breakdown of the TEA/LCA total cost into CAPEX and OPEX line items. The TEA/LCA provides total annual cost and notes amortization over 20 years, but investment and operating line-item structure is not extractable from the excerpts. Retrieval plan: access full TEA spreadsheet/supplement; request vendor EPC estimates for reactor/filtration/roaster; compare to the modeled reactor sizing example (198-gallon reactor for 100 tons/year).

- Solvent losses and solvent management requirements for D2EHPA/kerosene systems. The SX excerpt specifies D2EHPA concentration and stripping conditions but not solvent loss rates. Retrieval plan: pilot-scale mixer-settler or column trial with organic inventory tracking; solvent loss typically appears in HSE solvent-emissions plans and OPEX reagent makeup tables.

- Performance under realistic chelators, oils, surfactants, and coolant additives typical of grinding coolants and plating/finishing operations. The AMSS work demonstrates the magnitude of coolant fraction and uses roasting to remove it, but does not quantify organic interference in downstream separations. Retrieval plan: characterize TOC and specific additives in coolant and rinse waters; spike tests to quantify adsorption/SX performance impact at controlled compositions.

- Scale-up throughput for chromatography and adsorbent columns. Chromatography is reported at 50 µL injections and 1 mL/min flow, which is far from plant scale. Retrieval plan: translate to column capacity by measuring dynamic binding capacity and breakthrough curves at relevant superficial velocities; vendors’ column-resin datasheets and pilot skid specs typically provide these metrics.

- Selectivity coefficients (or separation factors) for Nd/Pr/Dy vs Fe/Co/B across technologies. SX reports co-extraction and stripping behavior in %, while adsorption reports Fe recovery; neither provides a unified selectivity coefficient in the excerpts. Retrieval plan: compute separation factors from measured distribution coefficients in controlled experiments and report with co-ion composition (Fe, Co, B).

- Energy intensity for high-temperature pretreatments in roasting-based manufacturing-waste flowsheets. Roasting temperatures and durations are given, and one TEA provides roasting energy intensity, but roasting energy is not consistently reported across routes. Retrieval plan: instrument roasters/furnaces for kWh per batch; energy reporting appears in TEA/LCA appendices and utility bills for thermal units.

- Impact of iron oxidation state control on downstream separations. One leachate route adds 0.1 vol.% H2SO4 after filtration “to prevent the oxidation of ferrous iron,” implying sensitivity to redox state. Retrieval plan: measure Fe(II)/Fe(III) speciation and its effect on extraction/adsorption; this is typically discussed in hydromet operating manuals and lab reports on PLS stability.

- Quantified benefit of physical pre-concentration on leaching residue and downstream reagent consumption. Flash reduction + magnetic separation reports REOs enrichment and qualitative residue avoidance, but does not (in excerpts) quantify downstream reagent savings or residue mass. Retrieval plan: run paired leach tests (with/without pre-concentration) and quantify residue mass, leach kinetics, and acid consumption; capture in pilot campaign reports.

- Applicability to electroplating/finishing effluent and rinse waters. None of the provided excerpts explicitly treats plating effluent or rinse waters. Retrieval plan: search and screen plating-effluent rare-earth removal studies; in-plant validation via composite sampling at plating rinse lines and bench adsorption/precipitation trials with co-ions (Ni, Cu, Zn) as present.

- Commercial vendor offerings for manufacturing-waste recovery (as opposed to EOL recycling plants). The excerpts include reagent suppliers and a manufacturer scrap source, but do not include turnkey vendor process datasheets for coolant/sludge/wastewater treatment. Retrieval plan: collect vendor technical datasheets and case studies; the fastest path is structured vendor calls requesting: treated flow (m³/day), inlet metals (mg/L), outlet metals (mg/L), resin/sorbent life, consumables, and installed cost basis; then validate via a short on-site trial using plant composite samples.

## Synthesis

The strongest quantitative benchmarks in the provided excerpts for manufacturing-waste-derived streams come from a bench D2EHPA solvent extraction route (99.9% Nd extraction; >99.7% Dy extraction) and a TEA/LCA-modeled acid-free dissolution route (overall REE extraction/recovery 96%–99%, baseline 97%). For wastewater-side removal, a bio-derived hydrogel adsorbent shows >93% recovery of Nd and Dy and reports Nd capacity of 125 mg/g with Fe recovery of 5.04%, suggesting promise for selective polishing but with missing discharge-style metrics in the excerpts. Across routes, the dominant hidden burdens are iron handling (filtration/precipitation and slow iron-removal kinetics), coolant/organic content (AMSS at 52.5% cooling reagent driving roasting pretreatment), and reagent circularity/loss (copper nitrate recycling efficiency ~70% and identified as an ecotoxicity driver). A biological approach plausibly “wins” if it maintains >93% Nd/Dy recovery with strong Fe rejection and multi-cycle stability (>85% capacity after five cycles), and “fails” if it cannot tolerate iron-rich matrices or coolant-laden streams without energy-intensive pretreatment comparable to oxidation roasting. The excerpts clearly identify where wastes originate (cutting/grinding swarf; grinding sludge; polishing scraps) but do not provide a direct, quantified description of the prevailing in-plant “do-nothing” baseline, so establishing a baseline should begin by mapping existing iron removal, coolant handling, and residue management practices against the unit operations explicitly described in the recovery flowsheets (e.g., CaCl2 + Ca(OH)2 iron removal; oxidation roasting for coolant removal; pre-concentration to avoid leach residues).