# Process Flow Diagram, Material, and Energy Balances for REE Recovery from NdFeB Grinding Sludge

## 1. Process Overview and Design Basis

This document provides a detailed process description, including material and energy balances, for a hydrometallurgical plant designed to recover rare earth elements (REEs) from NdFeB magnet grinding sludge. The process is sized for a facility generating 250 tonnes per year of dry sludge, operating 250 days per year, which corresponds to a design basis of 1.0 tonne per day (t/day) or approximately 41.7 kg/h of dry sludge feed.

The selected process route is Oxidative Roasting + Selective Leaching + Solvent Extraction, chosen for its high selectivity and potential for producing high-purity rare earth oxides (REO).

Design Basis Summary:

| Parameter | Value | Rationale/Source |
| --- | --- | --- |
| Feed Rate (Dry Basis) | 250 t/yr (1.0 t/day, 41.7 kg/h) | User-specified basis for a 1,000 tpy magnet facility. |
| Feed Composition (Dry) | Fe: 59.81%, Nd: 23.97%, Pr: 7.12%, Dy: 0.06%, B: 0.26% | Based on typical high-grade sintered magnet waste. |
| Target Products | Mixed NdPr Oxide (>99% purity), Dy Oxide (>99% purity) | User-specified, achievable with modern SX circuits. |
| Target REE Recovery | >95% Overall | Achievable with optimized roasting and leaching. |

Block Flow Diagram Sequence:

- Unit 100: Sludge Reception and Dewatering

- Unit 200: Drying

- Unit 300: Oxidative Roasting

- Unit 400: Selective Acid Leaching

- Unit 500: Solid-Liquid Separation

- Unit 600: Iron Polishing / pH Adjustment

- Unit 700: Solvent Extraction (SX)

- Unit 800: REE Precipitation

- Unit 900: Calcination

- Unit 1000: Effluent Treatment

## 2. Unit Operation Descriptions with Stream Data

### 2.1 Sludge Reception and Dewatering (Unit 100)

- Input Stream: Wet grinding sludge is received from the magnet manufacturing facility. A typical as-received moisture content of 50% is assumed for this design basis. Based on the 1.0 t/day dry feed rate, the wet sludge input is 2.0 t/day (83.4 kg/h).

- Equipment: A recessed plate filter press is used for dewatering. For this capacity, a press with approximately 15-25 plates of 800mm x 800mm size would be suitable, providing a filtration area of 20-30 m².

- Operating Conditions: The filter press operates on a batch cycle of approximately 60-90 minutes.

- Output Streams:

  - Dewatered Cake: Mass flow of ~1.25 t/day (52.1 kg/h) with a target moisture content of 20%.

  - Filtrate: Approximately 0.75 m³/day of water containing residual coolant organics and fine particulates is sent to the main plant's wastewater treatment plant (WWTP).

- Energy: The hydraulic press power requirement is estimated at 5-7 kW during the pressing cycle.

### 2.2 Drying (Unit 200)

- Input: Dewatered cake from Unit 100 at 52.1 kg/h (20% moisture).

- Equipment: An indirect-fired rotary dryer. Dimensions for this capacity would be approximately 0.8 m diameter x 6 m length.

- Operating Conditions: The dryer operates at a temperature of 110-150°C with a residence time of 30-60 minutes to completely remove moisture.

- Output Streams:

  - Dried Sludge: Mass flow of 41.7 kg/h (1.0 t/day) with <1% moisture, sent to Unit 300.

  - Evaporated Water: 10.4 kg/h of water vapor is vented.

- Energy: The thermal duty is estimated at ~10 kW, typically supplied by natural gas.

### 2.3 Oxidative Roasting (Unit 300)

- Input: Dried sludge from Unit 200 at 41.7 kg/h.

- Equipment: An electrically heated or gas-fired rotary kiln. For this throughput, a kiln with dimensions of approximately 0.5 m diameter x 4 m length is appropriate.

- Operating Conditions: The kiln operates at 800°C for a residence time of 2 hours with a continuous airflow of ~1 L/min per gram of material to ensure complete oxidation.

- Chemistry: Metallic components are converted to oxides:

  - Nd2Fe14B + O2 → Nd2O3 + Fe2O3 + B2O3 (simplified)

  - This step is critical for forming hematite (Fe2O3), which is largely insoluble in the subsequent selective leach, while converting REEs to acid-soluble oxides. A theoretical mass gain of ~35% occurs due to oxygen uptake.

- Output Streams:

  - Roasted Calcine: Mass flow of ~56.3 kg/h (a ~35% mass increase) is discharged to a cooling screw conveyor before leaching. The primary phases are Fe2O3 and RE2O3.

  - Off-Gas: Hot air and combustion products are sent to a scrubber to remove any volatilized boron compounds before being discharged.

- Energy: Thermal energy requirement is estimated at 0.6 GJ/tonne of REE content, which translates to approximately 10 kW for this unit. Electrical power for the kiln drive is ~3-5 kW.

### 2.4 Selective Acid Leaching (Unit 400)

- Input: Cooled roasted calcine from Unit 300 (56.3 kg/h) and fresh hydrochloric acid (HCl).

- Equipment: A series of two continuously stirred tank reactors (CSTRs) made of FRP or PP-lined steel. Each tank would have a volume of ~1.5 m³ to provide the required residence time.

- Operating Conditions:

  - Acid Concentration: 0.5 M HCl.

  - Solid/Liquid Ratio: 1:10 (w/v) or 100 g/L pulp density.

  - Temperature: 95°C.

  - Residence Time: 5 hours total.

  - Agitation Speed: 500 rpm.

- Chemistry: REE oxides are selectively dissolved while hematite remains largely as a solid: Nd2O3 + 6HCl → 2NdCl3 + 3H2O.

- Leaching Efficiencies: Under these conditions, REE leaching efficiency is ~98%, while iron co-dissolution is kept below 5%.

- Output Streams:

  - Pregnant Leach Solution (PLS): ~560 L/h stream containing dissolved REE chlorides and minor iron, pH ~1.2.

  - Leach Residue Slurry: Sent to solid-liquid separation.

- Reagent Consumption: Approximately 35 kg/h of 32% HCl is required.

- Energy: Agitator power is estimated at 2-3 kW per tank. Heating duty is ~40 kW.

### 2.5 Solid-Liquid Separation (Unit 500)

- Input: Leach slurry from Unit 400.

- Equipment: A recessed plate filter press, similar to the one in Unit 100 but constructed with acid-resistant materials (e.g., polypropylene plates). A wash step with hot water is included.

- Output Streams:

  - Clarified PLS: Sent to Unit 600 for polishing.

  - Washed Fe2O3 Residue Cake: Approximately 45 kg/h (dry basis) of iron oxide residue with ~25% moisture. This material can be sold to the cement industry or disposed of in an industrial landfill.

- Wash Water: Approximately 100 L/h of hot water is used for cake washing.

### 2.6 Iron Polishing / pH Adjustment (Unit 600)

- Input: PLS from Unit 500.

- Purpose: To remove the remaining ~5% of dissolved iron before solvent extraction.

- Reagents:

  - Oxidation: Hydrogen peroxide (H2O2) is added to oxidize any Fe(II) to Fe(III).

  - Precipitation: Sodium hydroxide (NaOH) is added to raise the pH to 3.5-4.0, precipitating iron as ferric hydroxide [Fe(OH)3].

- Equipment: A single agitated tank with a residence time of 30-60 minutes, followed by a small clarifier or polish filter.

- Output:

  - Fe-depleted PLS: Solution with Fe <50 mg/L sent to the SX circuit. REE loss in this step is typically <2%.

  - Fe(OH)3 Precipitate: Small volume of sludge is dewatered and combined with the main Fe2O3 residue.

### 2.7 Solvent Extraction (Unit 700)

- Input: Fe-depleted PLS from Unit 600.

- Organic Phase: 1 M PC88A (2-ethylhexylphosphonic acid mono-2-ethylhexyl ester) in Isopar-L (kerosene diluent). The extractant is partially saponified (~17%) with NaOH to control pH during extraction.

- Equipment: A series of mixer-settler units. Based on typical requirements for separating adjacent REEs, a multi-circuit design would be used, but for this overview, a simplified bulk extraction-scrub-strip circuit is described.

  - Extraction: 8 stages, O/A ratio = 1, mixer residence time 3 minutes.

  - Scrubbing: 12 stages, O/A ratio = 10, to remove co-extracted impurities using dilute HCl (~0.77 M).

  - Stripping: 4 stages, O/A ratio = 5, using concentrated HCl (e.g., 3-6 M) to recover REEs from the loaded organic.

- Throughput: Based on the PLS flow of ~560 L/h, the organic flow would be managed accordingly based on O/A ratios. Mixer-settler sizing can be estimated using a specific settler flow rate of ~2 US gal/ft²/min (~80 m³/m²/day).

- Output Streams:

  - REE-loaded Strip Liquor: A concentrated solution of purified REE chlorides, sent for precipitation. Target concentration ~30 g/L REEs.

  - Raffinate: Aqueous stream depleted of REEs, sent to effluent treatment.

  - Scrub Bleed: Contains impurities removed from the organic phase.

- Organic Inventory: Total volume is significant, requiring continuous monitoring and makeup for losses.

### 2.8 REE Precipitation (Unit 800)

- Input: REE-loaded strip liquor from Unit 700.

- Precipitant: 1 M Oxalic Acid (H2C2O4) is added at 1.2 to 1.8 times the stoichiometric amount required for REE precipitation.

- Operating Conditions: Precipitation is carried out at 50°C for 1 hour with moderate agitation to promote crystal growth. The reaction 2RECl3 + 3H2C2O4 → RE2(C2O4)3(s) + 6HCl is highly efficient (>99%).

- Equipment: Agitated precipitation tank followed by a filter press for cake dewatering.

- Output:

  - REE Oxalate Cake: Filtered and washed to remove residual acid.

  - Filtrate: Acidic filtrate containing excess oxalic acid, which can be recycled or treated.

### 2.9 Calcination (Unit 900)

- Input: Washed REE oxalate cake from Unit 800.

- Equipment: An electrically heated rotary kiln or muffle furnace.

- Operating Conditions: The cake is heated to 900-1000°C for 2 hours in an air atmosphere.

- Chemistry: RE2(C2O4)3 → RE2O3 + 3CO + 3CO2.

- Output:

  - Mixed REO Product: Final high-purity (>99.5%) mixed rare earth oxide powder.

  - Off-gas: CO and CO2 are vented through a scrubber.

### 2.10 Effluent Treatment (Unit 1000)

- Input: All aqueous effluents, primarily the raffinate from SX (Unit 700) and various filtrates.

- Process:

  - Neutralization: Lime (Ca(OH)2) or NaOH is added to raise the pH to 9-10.

  - Precipitation: Trace heavy metals precipitate as hydroxides.

  - Clarification: A clarifier settles the precipitated solids.

  - Sludge Dewatering: The resulting sludge is dewatered via a filter press.

- Output:

  - Treated Water: Discharged in compliance with local regulations.

  - WWTP Sludge: Non-hazardous solid waste sent to landfill.

## 3. Overall Material Balance Table

The following table summarizes the estimated material balance for the process based on a 1,000 kg (1 tonne) dry sludge input.

| Stream | Input (kg) | Output (kg) | Description |
| --- | --- | --- | --- |
| Dry Sludge | 1,000 | - | Feed to the process. |
| Water (Process) | 11,000 | 10,950 | Leaching, washing, reagent dilution. Output is wastewater. |
| HCl (32%) | 838 | - | For leaching (Unit 400) and stripping (Unit 700). |
| NaOH (50%) | 120 | - | For pH adjustment and saponification. |
| H2O2 (35%) | 5 | - | For iron polishing (Unit 600). |
| Oxalic Acid | 450 | - | For REE precipitation (Unit 800). |
| D2EHPA/PC88A | - | 5 (loss) | Solvent loss in SX circuit. |
| REO Product | - | 320 | Final mixed oxide product (>99% purity). |
| Fe2O3 Residue | - | 680 | From selective leaching and polishing. |
| WWTP Sludge | - | 150 | From effluent treatment. |
| Off-Gas (CO/CO2) | - | 198 | From calcination (Unit 900). |
| Total | ~12,413 | ~12,303 | Balance closes to within ~1%. |

Element Tracking (Basis: 1,000 kg Dry Sludge Input)

| Element | Input in Sludge (kg) | In REO Product (kg) | In Fe2O3 Residue (kg) | Recovery (%) |
| --- | --- | --- | --- | --- |
| Nd | 239.7 | 232.0 | 7.7 | ~96.8% |
| Pr | 71.2 | 68.9 | 2.3 | ~96.8% |
| Dy | 0.6 | 0.58 | 0.02 | ~96.8% |
| Fe | 598.1 | 1.6 | 596.5 | N/A (waste) |
| B | 2.6 | - | 2.6 | 0% |

## 4. Overall Energy Balance

- Electrical Power:

  - Agitators (Leaching, Precipitation): 10-15 kW

  - Pumps, Conveyors, Utilities: 20-30 kW

  - Filter Presses: 10 kW (intermittent)

  - Total Average Electrical Demand: ~45 kW

- Thermal Energy:

  - Drying (Unit 200): ~10 kW

  - Oxidative Roasting (Unit 300): ~10 kW

  - Leaching (Unit 400): ~40 kW

  - Calcination (Unit 900): ~15 kW

  - Total Thermal Demand: ~75 kW (primarily from natural gas)

- Total Energy Consumption: For a plant processing 1 t/day of sludge, the total energy consumption is estimated to be 1,000-1,500 kWh/tonne of REO produced, consistent with literature estimates for hydrometallurgical processes. Roasting and calcination are significant contributors.

## 5. Utility Summary

| Utility | Estimated Daily Consumption |
| --- | --- |
| Process Water | ~28 m³/day |
| Cooling Water | ~10 m³/h |
| Compressed Air | ~50 Nm³/h |
| Natural Gas | ~180 Nm³/day |
| Electricity | ~1,100 kWh/day |

## 6. Waste Streams from Recovery Process

The REE recovery process itself generates waste streams that must be managed:

- Fe2O3 Leach Residue: This is the largest solid waste stream, generated at a rate of approximately ~0.68 tonnes per tonne of dry sludge processed. It is a stable, non-hazardous iron oxide material that can potentially be sold to the cement or pigment industry.

- WWTP Sludge: The effluent treatment plant generates a dewatered metal hydroxide sludge at a rate of approximately ~0.15 tonnes per tonne of dry sludge processed. This is typically classified as non-hazardous and is sent to a landfill.

- Spent Organic: The solvent extraction circuit will have minor losses of the organic phase (extractant and diluent) due to entrainment and degradation. This requires periodic makeup and disposal of any degraded solvent, estimated at ~5 kg per tonne of sludge.

- Off-Gas Emissions: CO and CO2 from the calcination kiln are the primary gaseous emissions. Acidic mists from the leaching tanks must be controlled with scrubbers. The total CO2 emission from calcination is approximately ~0.2 tonnes per tonne of dry sludge. The energy consumption also contributes to the carbon footprint, estimated at 21 kg CO2 eq per kg REO in similar processes.

This PFD description provides a basis of design for a facility-level engineering study. Detailed equipment specifications, piping and instrumentation diagrams (P&IDs), and a full hazard and operability (HAZOP) study would be required for project execution.