# PART I: Technical Foundation — Manufacturing, Supply Chain, and Regulatory Framework

## Chapter 1

This chapter reproduces the full content of the main technical report on high-temperature permanent magnets for defense and security applications, including magnet types, manufacturing, machining waste, supply chain structure, competitive landscape, and qualification/testing requirements.

### Executive Summary

Defense and security systems rely on rare-earth permanent magnets as enabling components across major platforms, including the F-35 Lightning II, Virginia and Columbia class submarines, and unmanned aerial vehicles (UAVs). Reported platform-level demand is large, with the F-35 requiring more than 900 lb of rare earth elements (REEs), an Arleigh Burke DDG-51 destroyer requiring about 5,200 lb, and a Virginia class submarine needing about 9,200 lb, underscoring the strategic importance of secure supply chains for these materials and components.

For high-temperature operation, samarium-cobalt (SmCo) magnets (SmCo5 and Sm2Co17 families) are emphasized in the provided sources as preferred for high-temperature applications (e.g., 200–550 °C) because of their thermal stability and corrosion resistance. High-temperature NdFeB is positioned as a separate engineering path where coercivity is maintained at elevated temperatures (e.g., 150–200 °C) via heavy rare earth (HREE) additions (Dy/Tb) or via grain boundary diffusion processes that enhance coercivity without relying on bulk HREE loading.

Across both magnet types, the core industrial route described in the sources is powder metallurgy: alloy preparation, powder production, particle alignment and pressing, sintering and heat treatment, machining, and then magnetization. The machining and finishing step is consistently highlighted as the dominant source of material loss and scrap risk, with one public report stating machining recovery rates of 60–90% depending on final magnet complexity (i.e., 10–40% material becomes waste). The waste stream (magnet swarf) is described as often recycled back into process streams, and it can contain machine cutting fluids and magnetic powder because cutting is performed before magnetization.

From a defense supply-chain perspective, the sources emphasize that REE and critical material supply chains are global and multi-tiered, and that China dominates mining and processing stages for rare earths and other critical materials. U.S. policy and acquisition frameworks are tightening disclosure and sourcing requirements, including a DFARS-related expanded prohibition that GAO reports will go into effect on January 1, 2027, and a requirement for contractors to disclose the source of certain rare earth permanent magnets used in DoD systems.

### Magnet Types and Grades

SmCo and high-temperature NdFeB in the provided sources are presented less as commodity items and more as tightly specified engineering materials chosen to match elevated-temperature reliability requirements and environmental constraints. In defense and security contexts, these magnets sit in actuators, motors, and electromechanical subsystems within major platforms, contributing to the large REE usage cited for systems such as the F-35 and naval vessels/submarines.

SmCo grades. The sources describe SmCo magnets (SmCo5 and Sm2Co17) as offering “excellent hard magnetic properties, thermal stability, and corrosion resistance,” and as a preferred/ultimate choice for high-temperature applications (e.g., 200–550 °C). Reported performance ranges include a broad SmCo (BH)max range of 16–33 MGOe, reflecting variability across compositions and processing.

A specific grade example in the dataset is an Sm2O3-doped Sm2(Co,Fe,Cu,Zr)17 magnet reported as “EEC 2:17-27,” with (BH)max of 26–28 MGOe, intrinsic coercivity Hci of 34.1–36.1 kOe, and Br of 10.5–10.8 kGs. Commercial supplier data in the provided sources also lists VACOMAX SmCo properties including Br minimum values in the range 0.85–1.17 T (as presented), HcB minimum values around 600 kA/m (as presented), and typical (BH)max values in the range 160–265 kJ/m³ (20–33 MGOe), with maximum operating temperature stated as up to 350 °C for some alloys.

Thermal stability is further reflected in reversible temperature coefficient examples: a “standard Sm2Co17 magnet” is reported with a reversible temperature coefficient of about −350 ppm/K between room temperature and 200 °C, and SmCo5 is reported with RTC(Br) about −450 ppm/K.

High-temperature NdFeB and coercivity engineering. The sources describe a conventional high-temperature NdFeB approach of adding Dy/Tb to improve coercivity and avoid demagnetization at high operating temperatures (150–200 °C). One cited example (in a non-defense end-use context) reports that sintered NdFeB magnets used for wind turbines and electric/hybrid vehicle motors “usually contain about 10 wt% Dy/Tb,” illustrating the scale of HREE loading sometimes used to preserve coercivity at elevated temperatures.

A second approach emphasized in the dataset is grain boundary diffusion (GBD), described as a “well-established method” that “considerably enhances the coercivity” of sintered NdFeB and optimizes microstructures, including approaches using DyH3 nanoparticles (to fabricate “Dy-less” high-coercivity magnets) and diffusion sources such as DyCo alloys or Dy films deposited by magnetron sputtering. Quantitatively, one study reports that increasing diffusion temperature from 700 to 950 °C increased Hcj from 1339.3 to 1767.1 kA/m while Jr increased from 1.380 T to 1.439 T. Another report states that Dy diffusion with a primary diffusion heat treatment at 900 °C for 6 h increased coercivity from 1073 to 1418 kA/m versus the original magnet.

### Manufacturing Process Chain

The manufacturing chain described for sintered rare-earth magnets is dominated by powder metallurgy steps and high-temperature thermal processing, with the sources explicitly describing the general flow as alloy preparation, powder production, particle alignment and pressing, sintering and heat treatment, machining, and finally magnetizing. For SmCo specifically, one cited process statement describes manufacturing “by powder metallurgical technique involving isostatic pressing and sintering in inert atmosphere at temperatures range of 1140–1170 °C.”

Raw materials and powder production. Powder production routes in the sources include hydrogen decrepitation (HD), described as a process where a material absorbs hydrogen gas in its interstitial sites, as well as crushing/milling and jet milling routes for Sm2(Co,Fe,Cu,Zr)17 powders. One example reports Sm2(Co,Fe,Cu,Zr)17 powder prepared from book mold ingots by crushing and milling, then ground to an average particle size of about 7 ± 2 μm using an AFG jet mill.

Alignment and pressing. The sources show strong-field alignment as a critical step prior to compaction, including an example where blended powder mixtures were aligned using a 4 T pulsed magnetic field. Pressing approaches include isostatic pressing into green compacts, with one report citing approximately 240 MPa and another citing about 250 MPa after alignment in a magnetic field of 1300 kA/m.

Sintering, densification, and heat treatment. For SmCo sintering, the dataset includes a statement of inert-atmosphere sintering in the 1140–1170 °C range for powder-metallurgical routes. Another Sm2(Co,Fe,Cu,Zr)17 example reports sintering at about 1200 °C and holding slightly below sintering temperature for homogenization. Density is treated as a key acceptance/quality target, with one source stating that “the density [is required] to be > 95% of theoretical density.”

Post-sinter heat treatment is documented as multi-step thermal processing, including quenching and annealing at 850 °C followed by slow cooling to 400 °C at 0.7 K/min, a multi-hour hold, and a final quench in one reported Sm2(Co,Fe,Cu,Zr)17 route. The sources also emphasize that sintering and heat treatment cause substantial shrinkage that must be designed into tooling and machining allowances, reporting about 7–25% linear shrinkage overall and anisotropic shrinkage ranges of 17–25% parallel to the magnetic alignment direction and 7–13% perpendicular to it (depending on composition and sintering temperatures).

Diffusion processing for high-coercivity NdFeB. For high-temperature NdFeB, grain boundary diffusion is described in the sources as a route to produce high-performance magnets and to enhance coercivity and thermal stability, using diffusion sources including DyH3 nanoparticles, DyCo alloys for infiltration, and Dy films deposited by magnetron sputtering. The diffusion temperature dependence and coercivity improvements (e.g., 700–950 °C leading to Hcj 1339.3→1767.1 kA/m; or 900 °C/6 h yielding 1073→1418 kA/m) provide quantitative anchors for the thermal budgets involved in these processes.

Coatings and corrosion protection. The sources differentiate corrosion behavior by material family, noting that SmCo magnets are naturally corrosion resistant and that coating is often optional for SmCo in some applications. For NdFeB, a coating specification reference lists Ni-Cu-Ni (standard triple layer) with a temperature note of ~200 °C, indicating the kinds of coatings referenced for neodymium magnets in higher-temperature environments.

### Machining, Finishing, and Waste Generation

The sources consistently identify machining as both a major technical risk (brittleness-driven fracture and chipping) and the dominant stage for material loss when converting sintered blocks into end-use geometries. A general process description states that after sintering and heat treatment, magnets are machined and then magnetized, which also aligns with the description that cutting is performed before magnetization in the context of swarf generation.

How parts are finished and delivered. For sintered rare-earth magnets in general, one source describes that “finished magnets are then machined” using wire saws, wire electrical discharge machining (EDM), or abrasive wheel slitting machines, implying that suppliers can deliver machined/finished geometries rather than only sintered blocks. The same overarching process description places magnetization after machining, which is consistent with the machining-before-magnetization statement in the NdFeB supply chain report’s swarf discussion.

Methods and tolerances. For high-precision shaping, wire EDM is highlighted in the provided sources as enabling tight tolerances, with one tolerance reference stating that wire EDM can achieve tolerances in the range of ±0.005 mm to ±0.02 mm. Surface grinding is also described as a common finishing step for sintered magnets to achieve precise dimensions, with tolerances typically in the range of ±0.02 mm to ±0.05 mm.

Kerf and gap mechanics in wire EDM are quantified in the provided sources, including a reported wire-workpiece gap usually ranging from 0.025 to 0.075 mm. Kerf stability is described in one experimental study as having standard deviation in the range of 1.1–3.1 μm across a set of 27 cuts, and the same source provides an empirical mean kerf relationship K_m(μm) = 0.203·V + 104 (as reported).

Waste and scrap mechanisms. Material loss is described as being greatest during machining of the sintered block into end-use geometries; a U.S. public report states that machining has a recovery rate of 60–90% depending on size and complexity of the final magnet, implying 10–40% waste during machining for many geometries. That same report notes that although considerable material is lost, the resulting waste (magnet swarf) is often recycled and returns to the process flow stream.

SmCo introduces an additional scrap driver due to brittleness. One source attributes “magnet production loss of up to 20–30% in volume” to brittleness effects, and a separate processing reference describes Sm-Co magnets as the most brittle with machining failure rate up to 20%. In a wire EDM example, 1 of 7 reference magnets (about 14.3%) had fracture problems while preparing rectangular bars, illustrating the brittleness-driven yield risk in finishing operations.

Waste stream forms and composition. The NdFeB magnet supply chain report provides a global-scale estimate that the volume of the swarf recycling stream in 2020 was about 9% of NdFeB magnets produced globally. That report further notes that swarf streams “can contain some machine cutting fluids and magnetic powder,” and explicitly links this to the fact that cutting is performed before magnetization.

Waste generation summary. The table below consolidates the waste-related quantitative points that are explicitly stated in the provided sources.

| Waste and scrap metric | Reported value | Context and notes |
| --- | --- | --- |
| Machining recovery rate | 60–90% recovery (10–40% waste) | Described as the greatest material loss step when machining sintered blocks to end-use specifications, varying with size and complexity. |
| SmCo production loss linked to brittleness | Up to 20–30% volume loss | Attributed to brittleness in SmCo-based magnets in one report. |
| Sm-Co machining failure rate | Up to 20% | Described as a machining failure rate for brittle Sm-Co magnets in a manufacturing process reference. |
| WEDM fracture example | ~14.3% (1 of 7) fracture problems | Example observed during wire EDM preparation of SmCo bars for bending tests. |
| NdFeB swarf stream (global, 2020) | ~9% of production | Framed as the swarf recycling stream volume estimate in 2020 for NdFeB magnets globally. |
| Swarf composition indicator | Cutting fluids + magnetic powder possible | Explained as a consequence of cutting being performed before magnetization. |

### Supply Chain Structure and Logistics

The supply chain for rare earths and other critical materials relevant to permanent magnets is described by GAO as spread across the globe, with China dominating the mining and processing stages, and as a complex multi-tier process from raw material in the ground to a DoD weapon system. In response, DoD is reported to be actively working to establish a “Mine-to-Magnet” supply chain for rare earth materials, and GAO reports approximately $439 million in DoD awards since 2020 to vendors to reestablish domestic rare earth supply chains.

Supply chain flow. A defense-relevant “raw material to installed component” flow, using phrasing and step ordering described in the sources, can be expressed as:

Mining and extraction → separation to high-purity oxides/metals → alloy preparation → powder production (including routes such as hydrogen decrepitation) → particle alignment and pressing → sintering and heat treatment → machining → magnetization → lot qualification and inspection → delivery/installation into defense subsystems.

Within the manufacturing portion of this chain, specific operations are documented with quantitative anchors such as isostatic pressing around 240–250 MPa after magnetic alignment, and sintering regimes such as 1140–1170 °C (SmCo, inert atmosphere) or about 1200 °C (reported Sm2(Co,Fe,Cu,Zr)17 example), followed by multi-step heat treatments (e.g., 850 °C anneal and controlled cool to 400 °C).

Defense traceability and sourcing pressures. GAO reports that DoD completed DFARS rulemaking for an expanded prohibition that will go into effect on January 1, 2027, and that DoD will have to require contractors to disclose the source of certain rare earth permanent magnets used in DoD systems. In addition, the Federal Register text cited in the provided sources notes that DFARS authorizes DoD to issue individual and class nonavailability determinations if compliant materials are unavailable (DFARS 225.7018-4). The same Federal Register excerpt explicitly references “recycled NdFeB magnets milled and sintered in the United States,” indicating that U.S.-processed recycled feedstock is contemplated within DFARS discussions of compliant sourcing pathways.

Logistics implications of machining waste. The sources indicate that machining creates substantial swarf streams that are often recycled, and that these streams can contain cutting fluids and magnetic powder, implying that collection, storage, and handling logistics must manage both metallic/magnetic solids and process fluids. Because machining is described as the “greatest material loss” step and because recovery rate varies (60–90%), the magnitude of swarf handling and potential recycling flows is sensitive to end-use geometry complexity and tolerance requirements.

### Competitive Landscape and Certifications

The competitive landscape in the provided sources highlights a mix of specialized magnet manufacturers and vertically integrated magnetic-materials companies, with supplier differentiation frequently expressed in terms of in-house alloy/powder capability, machining/assembly capability, and ability to meet defense compliance expectations such as ITAR registration and AS9100 quality management systems. In parallel, broader policy and market context emphasizes that the United States imports large percentages of some extracted and processed critical mineral resources and related products, framing the business case for domestic capacity expansions and “mine-to-magnet” initiatives.

The table below summarizes defense-relevant attributes that are explicitly stated in the provided sources.

| Company | What they do (as stated in sources) | Defense-relevant compliance and quality indicators | Notes on integration and capability |
| --- | --- | --- | --- |
| Electron Energy Corporation (EEC) | Specializes in RECo5 and RE2TM17 type sintered magnets. Purchases pure raw materials (Sm, Co, Fe, Cu, Zr) for in-house production of SmCo 1:5 and 2:17 alloys. | ITAR compliant and DDTC registered. Certified to AS9100D and ISO 9001:2015. | Joined Magnetic Holdings, LLC (parent of Dexter and MCE). A press release describes this as creating a group of leading permanent magnet firms with a “vertically integrated manufacturing process” to create a robust and resilient supply chain. |
| Arnold Magnetic Technologies | Described as a U.S.-based industrial magnet manufacturer specializing in high-performance permanent magnets and assemblies for demanding markets such as aerospace and defense. Based in Rochester, NY with an operating history of over 130 years and serving aerospace and defense among other end-markets. | States that all locations in its RECOMA supply chain are registered with ITAR and can adhere to DFAR clauses. Lists ISO 9001:2015 and AS 9100 Rev D. | States it has established domestic supply chains for rare earth materials to ensure compliance with DoD requirements. A defense-facing example also cites its RECOMA 35E SmCo grade for 150–250 °C and high-speed applications (100,000 rpm+). |
| VACUUMSCHMELZE (VAC) | Described as one of the leading global manufacturers of advanced magnetic materials and related products. Provides VACOMAX SmCo material made from rare-earths and cobalt. | (No explicit ITAR/AS9100 statements in the provided quotes.) | States it has state-of-the-art facilities for further processing methods including wire-EDM. Announced an MoU with Ucore and e-VAC Magnetics to evaluate a collaborative supply agreement for high-purity rare earth oxides. |
| MP Materials | Described (in the provided source) as presenting a “mine-to-magnet story,” with NdPr metal online, trial sintered magnets running, and guidance to ~1,000 t/yr of finished magnets with a ramp beginning late 2025. | (No defense certifications in the provided quote.) | Positioned in the provided source as a domestic capacity expansion relevant to supply chain resilience for NdFeB magnets. |

### Qualification and Testing Requirements

The sources describe a qualification and acceptance ecosystem that combines magnetic property verification, dimensional and flux checks, materials and defect inspection, and environmental/corrosion testing tied to coatings and corrosion susceptibility. In defense procurement contexts, these technical requirements interact with compliance frameworks such as ITAR/DDTC registration and DFARS sourcing requirements and disclosures described by GAO and supplier statements.

Magnetic property qualification. A manufacturing process reference states that full second-quadrant demagnetization curves are required from a representative sample from each batch of magnets, and that a batch is typically defined as the load from the final heat treatment furnace. The same reference notes that it may also be necessary to measure side-to-side flux using a Hall probe and Gauss meter.

Magnetic measurement instrumentation and field levels in the provided sources include vibrating sample magnetometer (VSM) measurements with a maximum field of 9 T in one study, and demagnetization curve measurements using a permagraph with maximum applied field reported as 1500 kA/m after magnetization by a 6 T field in another report. A further source describes evaluation using a pulse-excitation-type BH tracer or a superconducting magnet-based VSM with magnetic field range of approximately 4775 kA·m⁻¹ (as stated).

For elevated-temperature magnetic measurements, an Arnold measurement white paper notes that some hysteresisgraphs have heated pole shoes or a heated sample holder enabling measurements up to +200 °C, and that a pulse field magnetometer (PFM) can measure magnetic properties in a temperature range of −40 to 220 °C (depending on the manufacturer).

Mechanical and defect inspection. Mechanical testing examples in the provided sources include flexural strength determination via three-point bending on an Instron 5944 universal test machine in one SmCo-focused study. Materials quality checks in a separate study include oxygen content measurement using an Eltra ON 900 oxygen/nitrogen analyzer and density measurement by Archimedes’ principle.

Non-destructive inspection is also described. One source states that applying ultrasonic testing (UT) allows users to analyze internal defects such as inclusions, porosity, and microcracks, and can identify locations of internal anomalies within Sm-Co sintered magnets. The same source argues UT can improve manufacturing efficiency and machinability, reduce scrap, and increase the use of what would be post-production waste while enhancing reuse and recycling at end-of-life disposition.

Corrosion, coatings, and environmental testing. The sources indicate corrosion susceptibility varies by magnet system, with one source stating “these magnets have a poor corrosion resistance and must be protected,” and reporting a salt spray test example using 5% NaCl solution continuously sprayed at 35 ± 2 °C for 72 hours on magnetized and demagnetized samples. Coating standards and methods are also cited: MIL-C-26074E requires that coated test specimens be exposed to neutral salt-spray testing in accordance with ASTM B117 for 100 hours for electroless nickel coatings (as stated in the cited document). Parylene is cited as a military specification conformal coating under MIL-I-46058.

Corrosion-performance impacts from diffusion processing are also referenced in the dataset, with one report stating that Tafel tests reveal Dy-diffused magnets have higher corrosion resistance with more positive equilibrium potential and lower corrosion current density (as described).

Compliance and sourcing requirements. Supplier certifications and registrations are explicitly cited in the dataset for U.S. defense-facing suppliers, including Arnold’s statements of ISO 9001:2015 and AS 9100 Rev D, and that all locations in its Samarium Cobalt RECOMA supply chain are registered with ITAR and can adhere to DFAR clauses. EEC likewise states ITAR compliance and DDTC registration and lists certification to AS9100D and ISO 9001:2015.

At the policy level, GAO reports DFARS rulemaking completion for an expanded prohibition effective January 1, 2027, and that DoD will have to require contractor disclosure of the source of certain rare earth permanent magnets used in DoD systems. The Federal Register excerpt cited in the dataset also notes DFARS authority for nonavailability determinations when compliant materials are unavailable (DFARS 225.7018-4).

### Gaps and Recommendations

The provided sources offer multiple explicit entry points for process-improvement and waste-management interventions, particularly at the machining stage where the largest reported material losses occur and where swarf streams can contain both cutting fluids and magnetic powders. They also explicitly describe inspection and testing practices (e.g., batch-defined demagnetization curves and UT for internal defects) that can be used to reduce scrap and support qualification confidence, which is directly relevant to both cost and sustainability in defense-grade supply chains.

A wastewater-focused provider targeting defense-grade magnet manufacturing can align offerings to the waste stream and compliance characteristics described in the sources. The following recommendations are grounded in the waste and testing descriptions explicitly cited.

- Prioritize treatment and separation solutions for swarf streams that may include cutting fluids and fine magnetic powders, because the NdFeB supply chain report explicitly states swarf “can contain” both cutting fluids and magnetic powder, and that cutting occurs before magnetization.

- Quantify and design for high variability in swarf volume driven by machining yield, because a public report states machining recovery ranges from 60–90% depending on magnet size and complexity (10–40% waste), and because SmCo brittleness can drive additional losses and failures (e.g., up to 20–30% volume loss attributed to brittleness in one source and up to 20% machining failure rates in another).

- Integrate inspection-enabled quality control offerings where appropriate, because UT is described as a method to locate internal anomalies such as inclusions, porosity, and microcracks in Sm-Co sintered magnets and as enabling reduced scrap and increased use of post-production waste and recycling opportunities.

DFARS-related disclosure and sourcing requirements described by GAO indicate that procurement teams should treat traceability and source documentation as schedule-critical deliverables, not merely contractual boilerplate. Supplier-facing recommendations supported by the provided sources include:

- Plan qualification around batch-based sampling defined by final heat treatment furnace loads and include full second-quadrant demagnetization curves and flux checks where needed, because these are explicitly described as batch-level requirements and practices in a manufacturing process reference.

- Where corrosion risk is material (e.g., in magnets described as having poor corrosion resistance), align coating selection and validation with salt-spray practices and military coating specifications cited in the sources (e.g., ASTM B117 salt-spray tests and MIL-C-26074E for electroless nickel; MIL-I-46058 for parylene).

Policy actions in the sources reinforce that defense magnet supply chains are a national priority, including DoD’s stated effort to establish a “Mine-to-Magnet” supply chain and the reported $439 million in awards since 2020 to reestablish domestic rare earth supply chains. Congressional proposals cited in the dataset further include bills directing DOE consortium research on REE extraction and establishing DoD grant programs authorizing $50 million per year for four years to encourage domestic development of critical minerals, reflecting sustained legislative interest in reducing vulnerability associated with globalized supply chains. Additional proposals would create federally chartered entities to mitigate high costs and radioactive byproducts potentially associated with REE extraction from minerals found with radioactive elements.

## Chapter 2

This chapter reproduces the full content of the waste-stream characterization report focused on machining swarf and sludge from NdFeB and SmCo magnet finishing operations, including waste fractions, swarf chemistry, particle sizes, fluid contamination, recycling routes, and wastewater implications.

### 1. Overview of Machining Waste Generation

The manufacturing of high-performance rare earth permanent magnets (REPMs) is a subtractive process that generates a substantial amount of waste, particularly during the final machining and finishing stages. Sintered magnet blocks cannot be produced to precise final shapes, necessitating extensive grinding, cutting, and shaping to meet the tight dimensional tolerances required for defense and high-technology applications. This machining waste, known as swarf or sludge, represents a significant material and economic loss, but also a valuable secondary resource for critical rare earth elements (REEs).

The fraction of raw material converted to waste varies widely depending on the final magnet geometry, with estimates ranging from 6% to as high as 73%. More commonly, manufacturing scrap, including swarf and cutting sludge, is reported to account for 20% to 30% of the starting alloy mass. This manufacturing waste is dominated by fine-particle sludge; in some analyses, sludge constitutes over 70% of the total waste generated. The global volume of this waste stream is significant, with the swarf recycled in 2020 estimated to be equivalent to 9% of the total NdFeB magnets produced globally that year. While defense-specific factors like tighter tolerances are understood to increase waste generation, quantitative data directly linking tolerance levels to a specific increase in waste fraction is not detailed in the available literature.

### 2. Swarf Chemical Composition

The chemical and phase composition of machining swarf is critical to its recycling potential. The swarf largely mirrors the composition of the parent magnet alloy but is heavily oxidized and contaminated with machining media.

NdFeB Swarf. Neodymium-Iron-Boron (NdFeB) swarf is a complex mixture containing valuable REEs and a high concentration of iron.

- Elemental Composition: NdFeB magnets contain approximately 30-32 wt.% REEs. Analysis of swarf and scrap material shows a composition of roughly 63-72 wt.% iron, 20-27 wt.% neodymium, 3-6 wt.% praseodymium, and 0.5-7 wt.% dysprosium, along with about 1 wt.% boron. Minor additions of cobalt (up to 5 wt.%), copper, aluminum, and niobium may also be present.

- Phase Composition: The primary magnetic phase in the swarf is Nd2Fe14B, which can account for 96-98% of the original magnet's structure. Swarf is also characterized by the presence of REE-rich grain boundary phases.

- Oxide Content: Swarf is heavily oxidized due to the high surface area of fine particles and exposure to air and cutting fluids. Oxygen content in recycled material can be as high as 2000–50,000 ppm, compared to 300-400 ppm in primary alloys. Oxidation leads to the decomposition of the primary Nd2Fe14B phase into various oxides, including Nd2O3, Fe2O3, and complex oxides like NdFeO3.

SmCo Swarf. Samarium-Cobalt (SmCo) swarf is characterized by high concentrations of samarium and cobalt, with a simpler REE profile than NdFeB.

- Elemental Composition: The composition varies based on the alloy stoichiometry (SmCo5 or Sm2Co17). SmCo5 alloys contain approximately 36 wt.% REEs (primarily Sm) and 63 wt.% Co. Sm2Co17 alloys contain around 25 wt.% Sm, 60-70 wt.% Co, and significant additions of iron (10-15 wt.%), copper (5-10 wt.%), and zirconium. One detailed analysis of Sm2Co17 scrap powder found 42.3 wt.% Co, 22.8 wt.% Sm, and 22.4 wt.% Fe.

- Phase Composition: The dominant phases in SmCo swarf are intermetallic compounds such as Sm2Co17 and FeCo.

### 3. Particle Size Distributions

Machining processes like grinding and cutting generate swarf with a wide range of particle sizes, which significantly impacts handling, oxidation, and recycling efficiency.

- Milled Powders: Studies involving planetary ball milling of NdFeB scrap show a progressive reduction in particle size with time. The median particle diameter (d50) can be reduced from over 20 μm to below 5 μm after 15 hours of grinding. The d90 value (representing the coarsest 10% of particles) can decrease from over 65 μm to around 10 μm in the same timeframe.

- Hydrogen Processed Powders: Hydrogen decrepitation (HD) produces a friable powder with particle sizes typically ranging from 6 μm to 600 μm. The more advanced Hydrogenation-Disproportionation-Desorption-Recombination (HDDR) process results in much finer, nanograined powders with grain sizes around 300 nm.

- Sieved Fractions: In recycling workflows, specific mesh sizes are used for separation. Powders are often sieved to <90 μm or <45 μm for processing. For example, sieving hydrogen-processed powder at 90 μm can effectively separate the brittle magnet material from ductile nickel coatings.

### 4. Cutting Fluid Contamination

Machining sludge is inherently contaminated with the fluids used as coolants and lubricants during grinding and cutting operations. This contamination complicates recycling by introducing organic and inorganic impurities.

- Fluid Composition: A common type of coolant is a water-miscible, mineral oil-based fluid, such as Mobilcut 230. This type of fluid can contain mineral oil, boric acid (10-20 wt.%), ethanol (1-5 wt.%), and various oleates and oils. Ethanol is also used as a grinding medium to reduce friction and prevent surface oxidation.

- Contamination Levels: The amount of residual coolant in grinding slurries can be substantial, varying from less than 1% to over 20% by weight. This contamination introduces unwanted elements, primarily carbon and additional oxygen, which can interfere with metallurgical recovery processes.

- Removal: Pre-treatment steps are often required to remove these organic impurities. This can include washing with solvents like acetone or thermal pre-conditioning via pyrolysis to volatilize the organic compounds before melting. Pyrolysis at 600°C for 15 minutes has been shown to reduce volatiles to below detectable limits.

### 5. Rare Earth Recovery Processes and Yields

A variety of metallurgical techniques have been developed to recover REEs and other valuable metals like cobalt from magnet swarf. These can be broadly categorized into hydrometallurgical, pyrometallurgical, and hydrogen-based routes.

Hydrometallurgical Routes. Hydrometallurgy, which uses aqueous solutions to leach and separate metals, is a flexible and widely studied approach for REE recovery, capable of producing high-purity products.

- Leaching: The first step involves dissolving the swarf in an acid. Strong mineral acids like sulfuric acid (H2SO4), hydrochloric acid (HCl), and nitric acid (HNO3) are commonly used. This process can achieve high leaching efficiencies, often exceeding 95-99% for REEs. However, it often co-dissolves large amounts of iron, complicating downstream separation. Alternative "greener" reagents like organic acids (citric acid) and acid-free copper salt solutions are also being explored.

- Separation and Purification: After leaching, the REEs are separated from iron and other impurities. This is typically done through selective precipitation (using agents like oxalic acid or sodium sulfate) or solvent extraction. Solvent extraction uses organic chemicals like D2EHPA mixed with kerosene to selectively pull REEs from the aqueous solution.

- Recovery Yields: Laboratory-scale hydrometallurgical processes report high recovery rates. For example, various studies have demonstrated REE recovery efficiencies of 97-99%. Element-specific recoveries can be very high, with some processes achieving >98% for Nd, >98% for Pr, and >97% for Dy.

Pyrometallurgical Routes. Pyrometallurgy uses high temperatures to smelt, refine, and separate metals. These methods are often faster and can handle larger capacities than hydrometallurgical routes.

- Methods: Common techniques include liquid metal extraction (using molten magnesium or copper to selectively dissolve REEs), molten salt extraction (using chloride or fluoride salts), and oxidative slagging (where REEs are oxidized and collected in a slag phase). Temperatures for these processes range from 700°C to over 1500°C.

- Recovery Yields: Pyrometallurgical methods can also achieve high recovery. Liquid magnesium extraction has shown nearly 100% efficiency for Nd, though lower for Dy (~60%). Molten MgCl2 extraction has recovered ~80% of Nd and Dy. Oxidative smelting followed by leaching has demonstrated >99% overall REE recovery in some studies.

Hydrogen Processing. Hydrogen-based processes use hydrogen gas to break down the brittle magnet material into a powder, facilitating separation and direct recycling.

- Methods: The two main techniques are Hydrogen Decrepitation (HD) and Hydrogenation-Disproportionation-Desorption-Recombination (HDDR). HD uses hydrogen at or near room temperature to create a friable, demagnetized powder. HDDR is a more complex process involving higher temperatures (750-950°C) that produces a fine, anisotropic powder suitable for high-performance bonded or re-sintered magnets.

- Recovery Yields: These "short-loop" recycling methods are highly efficient in terms of material recovery, with processes like HPMS (Hydrogen Processing of Magnet Scrap) reporting recovery rates of 90-98% for the magnetic alloy powder.

### 6. SmCo Waste Streams

While much of the recycling research focuses on NdFeB magnets, SmCo magnets are critical for high-temperature defense applications, and their waste streams are also a valuable source of cobalt and samarium.

- Composition: SmCo swarf composition depends on the alloy type. SmCo5 alloys contain roughly 36 wt.% REEs (mostly Sm) and 63 wt.% Co. The more common high-temperature Sm2Co17 grades contain ~25 wt.% Sm, 60-70 wt.% Co, and significant amounts of Fe (10-15 wt.%), Cu (5-10 wt.%), and Zr. One detailed analysis of Sm2Co17 scrap powder reported 42.3 wt.% Co, 22.8 wt.% Sm, and 22.4 wt.% Fe.

- Recovery Processes: Recycling of SmCo is considered simpler than NdFeB due to the less complex mixture of REEs. Hydrometallurgical routes are common, using acids like HNO3 or H2SO4 to leach the metals. Selective leaching can be effective; for example, oxidative leaching with 3M HNO3 at 60°C achieved 99% dissolution of Sm and Co while leaving iron as a solid residue.

- Recovery Yields: Studies have demonstrated high recovery efficiencies for both samarium and cobalt. One process reported >98% recovery of Sm with >99% purity. Another achieved precipitation efficiencies of 98.7% for Sm and 96.2% for Co. Microwave-assisted acid digestion has also shown quantitative recovery (>95%) of all elements from SmCo waste.

### 7. Commercial Recycling Landscape

While much of the research on REE magnet recycling remains at the laboratory or pilot scale, a growing number of companies are commercializing these technologies.

- Urban Mining Company (Noveon Magnetics): Based in Texas, this company uses a hydrogen-based process (Magnet-to-Magnet) to recycle scrap magnets directly into new, high-performance sintered NdFeB magnets.

- Cyclic Materials: A Canadian company that has developed a hydrometallurgical process to recover REEs, as well as copper, steel, and aluminum, from magnetic waste streams.

- HyProMag: A UK-based company (with operations in Germany and the US) commercializing the HPMS process developed at the University of Birmingham. They are focused on producing recycled NdFeB alloy powders for new magnet production, with a pilot plant operational and larger facilities planned.

- Other Players: Other notable entities include Momentum Technologies (licensing a membrane-assisted solvent extraction process from Oak Ridge National Laboratory), TdVib LLC (licensing an acid-free dissolution process from Ames Laboratory), and established chemical companies like Solvay that are involved in REE recovery from various waste streams. In China, companies like Ganzhou YouLi Technology and Ji’an XinTai Technology use conventional hydrometallurgical routes for REO recovery.

### 8. Implications for Wastewater Treatment

The hydrometallurgical recycling of magnet swarf generates significant wastewater streams that require specialized treatment. These streams are typically acidic and contain high concentrations of dissolved metals and process chemicals.

- Wastewater Composition: The primary liquid waste is the “pregnant leach solution” (PLS) after the initial acid leaching step. Analysis of a PLS from NdFeB waste shows high concentrations of dissolved metals, including iron (up to 62.9 g/L), neodymium (20.5 g/L), and dysprosium (6.4 g/L), along with other elements like cobalt, boron, and praseodymium in the g/L range.

- pH and Chemical Load: The wastewater is highly acidic, with a final pH often between 1.0 and 3.0 after leaching. The process consumes large volumes of strong acids (H2SO4, HCl, HNO3), bases (caustics), and precipitating agents like oxalic acid. The final effluent can contain residual salts such as ammonium chloride and ammonium nitrate from pH adjustment steps.

- Treatment Challenges and Opportunities: A key treatment step is the removal of iron, which is the most abundant metal. This is often done by raising the pH to precipitate iron as a hydroxide or jarosite. This process itself requires careful pH control and the addition of chemicals like calcium hydroxide. The resulting wastewater still contains dissolved REEs and other metals that must be recovered or removed. The high chemical load and complex metal mixture present a challenge for conventional wastewater treatment but also an opportunity for technologies that can selectively recover valuable elements from these dilute, complex streams. The economic viability of hydrometallurgical recycling is heavily dependent on the cost of wastewater treatment and the ability to recycle process chemicals like solvents and acids.

### Duplicate reproduction of the same report text

# Machining Waste Stream Characterization for Defense-Grade Rare Earth Permanent Magnets

## 1. Overview of Machining Waste Generation

The manufacturing of high-performance rare earth permanent magnets (REPMs) is a subtractive process that generates a substantial amount of waste, particularly during the final machining and finishing stages. Sintered magnet blocks cannot be produced to precise final shapes, necessitating extensive grinding, cutting, and shaping to meet the tight dimensional tolerances required for defense and high-technology applications. This machining waste, known as swarf or sludge, represents a significant material and economic loss, but also a valuable secondary resource for critical rare earth elements (REEs).

The fraction of raw material converted to waste varies widely depending on the final magnet geometry, with estimates ranging from 6% to as high as 73%. More commonly, manufacturing scrap, including swarf and cutting sludge, is reported to account for 20% to 30% of the starting alloy mass. This manufacturing waste is dominated by fine-particle sludge; in some analyses, sludge constitutes over 70% of the total waste generated. The global volume of this waste stream is significant, with the swarf recycled in 2020 estimated to be equivalent to 9% of the total NdFeB magnets produced globally that year. While defense-specific factors like tighter tolerances are understood to increase waste generation, quantitative data directly linking tolerance levels to a specific increase in waste fraction is not detailed in the available literature.

## 2. Swarf Chemical Composition

The chemical and phase composition of machining swarf is critical to its recycling potential. The swarf largely mirrors the composition of the parent magnet alloy but is heavily oxidized and contaminated with machining media.

### NdFeB Swarf

Neodymium-Iron-Boron (NdFeB) swarf is a complex mixture containing valuable REEs and a high concentration of iron.

- Elemental Composition: NdFeB magnets contain approximately 30-32 wt.% REEs. Analysis of swarf and scrap material shows a composition of roughly 63-72 wt.% iron, 20-27 wt.% neodymium, 3-6 wt.% praseodymium, and 0.5-7 wt.% dysprosium, along with about 1 wt.% boron. Minor additions of cobalt (up to 5 wt.%), copper, aluminum, and niobium may also be present.

- Phase Composition: The primary magnetic phase in the swarf is Nd2Fe14B, which can account for 96-98% of the original magnet's structure. Swarf is also characterized by the presence of REE-rich grain boundary phases.

- Oxide Content: Swarf is heavily oxidized due to the high surface area of fine particles and exposure to air and cutting fluids. Oxygen content in recycled material can be as high as 2000–50,000 ppm, compared to 300-400 ppm in primary alloys. Oxidation leads to the decomposition of the primary Nd2Fe14B phase into various oxides, including Nd2O3, Fe2O3, and complex oxides like NdFeO3.

### SmCo Swarf

Samarium-Cobalt (SmCo) swarf is characterized by high concentrations of samarium and cobalt, with a simpler REE profile than NdFeB.

- Elemental Composition: The composition varies based on the alloy stoichiometry (SmCo5 or Sm2Co17). SmCo5 alloys contain approximately 36 wt.% REEs (primarily Sm) and 63 wt.% Co. The more common high-temperature Sm2Co17 grades contain ~25 wt.% Sm, 60-70 wt.% Co, and significant additions of iron (10-15 wt.%), copper (5-10 wt.%), and zirconium. One detailed analysis of Sm2Co17 scrap powder reported 42.3 wt.% Co, 22.8 wt.% Sm, and 22.4 wt.% Fe.

- Phase Composition: The dominant phases in SmCo swarf are intermetallic compounds such as Sm2Co17 and FeCo.

## 3. Particle Size Distributions

Machining processes like grinding and cutting generate swarf with a wide range of particle sizes, which significantly impacts handling, oxidation, and recycling efficiency.

- Milled Powders: Studies involving planetary ball milling of NdFeB scrap show a progressive reduction in particle size with time. The median particle diameter (d50) can be reduced from over 20 μm to below 5 μm after 15 hours of grinding. The d90 value (representing the coarsest 10% of particles) can decrease from over 65 μm to around 10 μm in the same timeframe.

- Hydrogen Processed Powders: Hydrogen decrepitation (HD) produces a friable powder with particle sizes typically ranging from 6 μm to 600 μm. The more advanced Hydrogenation-Disproportionation-Desorption-Recombination (HDDR) process results in much finer, nanograined powders with grain sizes around 300 nm.

- Sieved Fractions: In recycling workflows, specific mesh sizes are used for separation. Powders are often sieved to <90 μm or <45 μm for processing. For example, sieving hydrogen-processed powder at 90 μm can effectively separate the brittle magnet material from ductile nickel coatings.

## 4. Cutting Fluid Contamination

Machining sludge is inherently contaminated with the fluids used as coolants and lubricants during grinding and cutting operations. This contamination complicates recycling by introducing organic and inorganic impurities.

- Fluid Composition: A common type of coolant is a water-miscible, mineral oil-based fluid, such as Mobilcut 230. This type of fluid can contain mineral oil, boric acid (10-20 wt.%), ethanol (1-5 wt.%), and various oleates and oils. Ethanol is also used as a grinding medium to reduce friction and prevent surface oxidation.

- Contamination Levels: The amount of residual coolant in grinding slurries can be substantial, varying from less than 1% to over 20% by weight. This contamination introduces unwanted elements, primarily carbon and additional oxygen, which can interfere with metallurgical recovery processes.

- Removal: Pre-treatment steps are often required to remove these organic impurities. This can include washing with solvents like acetone or thermal pre-conditioning via pyrolysis to volatilize the organic compounds before melting. Pyrolysis at 600°C for 15 minutes has been shown to reduce volatiles to below detectable limits.

## 5. Rare Earth Recovery Processes and Yields

A variety of metallurgical techniques have been developed to recover REEs and other valuable metals like cobalt from magnet swarf. These can be broadly categorized into hydrometallurgical, pyrometallurgical, and hydrogen-based routes.

### Hydrometallurgical Routes

Hydrometallurgy, which uses aqueous solutions to leach and separate metals, is a flexible and widely studied approach for REE recovery, capable of producing high-purity products.

- Leaching: The first step involves dissolving the swarf in an acid. Strong mineral acids like sulfuric acid (H2SO4), hydrochloric acid (HCl), and nitric acid (HNO3) are commonly used. This process can achieve high leaching efficiencies, often exceeding 95-99% for REEs. However, it often co-dissolves large amounts of iron, complicating downstream separation. Alternative "greener" reagents like organic acids (citric acid) and acid-free copper salt solutions are also being explored.

- Separation and Purification: After leaching, the REEs are separated from iron and other impurities. This is typically done through selective precipitation (using agents like oxalic acid or sodium sulfate) or solvent extraction. Solvent extraction uses organic chemicals like D2EHPA mixed with kerosene to selectively pull REEs from the aqueous solution.

- Recovery Yields: Laboratory-scale hydrometallurgical processes report high recovery rates. For example, various studies have demonstrated REE recovery efficiencies of 97-99%. Element-specific recoveries can be very high, with some processes achieving >98% for Nd, >98% for Pr, and >97% for Dy.

### Pyrometallurgical Routes

Pyrometallurgy uses high temperatures to smelt, refine, and separate metals. These methods are often faster and can handle larger capacities than hydrometallurgical routes.

- Methods: Common techniques include liquid metal extraction (using molten magnesium or copper to selectively dissolve REEs), molten salt extraction (using chloride or fluoride salts), and oxidative slagging (where REEs are oxidized and collected in a slag phase). Temperatures for these processes range from 700°C to over 1500°C.

- Recovery Yields: Pyrometallurgical methods can also achieve high recovery. Liquid magnesium extraction has shown nearly 100% efficiency for Nd, though lower for Dy (~60%). Molten MgCl2 extraction has recovered ~80% of Nd and Dy. Oxidative smelting followed by leaching has demonstrated >99% overall REE recovery in some studies.

### Hydrogen Processing

Hydrogen-based processes use hydrogen gas to break down the brittle magnet material into a powder, facilitating separation and direct recycling.

- Methods: The two main techniques are Hydrogen Decrepitation (HD) and Hydrogenation-Disproportionation-Desorption-Recombination (HDDR). HD uses hydrogen at or near room temperature to create a friable, demagnetized powder. HDDR is a more complex process involving higher temperatures (750-950°C) that produces a fine, anisotropic powder suitable for high-performance bonded or re-sintered magnets.

- Recovery Yields: These "short-loop" recycling methods are highly efficient in terms of material recovery, with processes like HPMS (Hydrogen Processing of Magnet Scrap) reporting recovery rates of 90-98% for the magnetic alloy powder.

## 6. SmCo Waste Streams

While much of the recycling research focuses on NdFeB magnets, SmCo magnets are critical for high-temperature defense applications, and their waste streams are also a valuable source of cobalt and samarium.

- Composition: SmCo swarf composition depends on the alloy type. SmCo5 alloys contain roughly 36 wt.% REEs (mostly Sm) and 63 wt.% Co. The more common high-temperature Sm2Co17 grades contain ~25 wt.% Sm, 60-70 wt.% Co, and significant amounts of Fe (10-15 wt.%), Cu (5-10 wt.%), and Zr. One detailed analysis of Sm2Co17 scrap powder reported 42.3 wt.% Co, 22.8 wt.% Sm, and 22.4 wt.% Fe.

- Recovery Processes: Recycling of SmCo is considered simpler than NdFeB due to the less complex mixture of REEs. Hydrometallurgical routes are common, using acids like HNO3 or H2SO4 to leach the metals. Selective leaching can be effective; for example, oxidative leaching with 3M HNO3 at 60°C achieved 99% dissolution of Sm and Co while leaving iron as a solid residue.

- Recovery Yields: Studies have demonstrated high recovery efficiencies for both samarium and cobalt. One process reported >98% recovery of Sm with >99% purity. Another achieved precipitation efficiencies of 98.7% for Sm and 96.2% for Co. Microwave-assisted acid digestion has also shown quantitative recovery (>95%) of all elements from SmCo waste.

## 7. Commercial Recycling Landscape

While much of the research on REE magnet recycling remains at the laboratory or pilot scale, a growing number of companies are commercializing these technologies.

- Urban Mining Company (Noveon Magnetics): Based in Texas, this company uses a hydrogen-based process (Magnet-to-Magnet) to recycle scrap magnets directly into new, high-performance sintered NdFeB magnets.

- Cyclic Materials: A Canadian company that has developed a hydrometallurgical process to recover REEs, as well as copper, steel, and aluminum, from magnetic waste streams.

- HyProMag: A UK-based company (with operations in Germany and the US) commercializing the HPMS process developed at the University of Birmingham. They are focused on producing recycled NdFeB alloy powders for new magnet production, with a pilot plant operational and larger facilities planned.

- Other Players: Other notable entities include Momentum Technologies (licensing a membrane-assisted solvent extraction process from Oak Ridge National Laboratory), TdVib LLC (licensing an acid-free dissolution process from Ames Laboratory), and established chemical companies like Solvay that are involved in REE recovery from various waste streams. In China, companies like Ganzhou YouLi Technology and Ji’an XinTai Technology use conventional hydrometallurgical routes for REO recovery.

## 8. Implications for Wastewater Treatment

The hydrometallurgical recycling of magnet swarf generates significant wastewater streams that require specialized treatment. These streams are typically acidic and contain high concentrations of dissolved metals and process chemicals.

- Wastewater Composition: The primary liquid waste is the “pregnant leach solution” (PLS) after the initial acid leaching step. Analysis of a PLS from NdFeB waste shows high concentrations of dissolved metals, including iron (up to 62.9 g/L), neodymium (20.5 g/L), and dysprosium (6.4 g/L), along with other elements like cobalt, boron, and praseodymium in the g/L range.

- pH and Chemical Load: The wastewater is highly acidic, with a final pH often between 1.0 and 3.0 after leaching. The process consumes large volumes of strong acids (H2SO4, HCl, HNO3), bases (caustics), and precipitating agents like oxalic acid. The final effluent can contain residual salts such as ammonium chloride and ammonium nitrate from pH adjustment steps.

- Treatment Challenges and Opportunities: A key treatment step is the removal of iron, which is the most abundant metal. This is often done by raising the pH to precipitate iron as a hydroxide or jarosite. This process itself requires careful pH control and the addition of chemicals like calcium hydroxide. The resulting wastewater still contains dissolved REEs and other metals that must be recovered or removed. The high chemical load and complex metal mixture present a challenge for conventional wastewater treatment but also an opportunity for technologies that can selectively recover valuable elements from these dilute, complex streams. The economic viability of hydrometallurgical recycling is heavily dependent on the cost of wastewater treatment and the ability to recycle process chemicals like solvents and acids.

## Chapter 3

This chapter reproduces the full content of the DFARS compliance pathway report, including definitions of covered materials and countries, the phased implementation through 2026 and the expanded prohibition effective January 1, 2027, nonavailability determination procedures, recycled NdFeB exceptions, domestic capacity initiatives, and GAO-identified compliance gaps.

### Regulatory Overview

The U.S. Department of Defense (DoD) regulates the procurement of rare earth permanent magnets through a framework designed to strengthen the domestic industrial base and reduce reliance on foreign supply chains. This regulatory structure is primarily implemented through the Defense Federal Acquisition Regulation Supplement (DFARS), with its authority stemming from legislative mandates in various National Defense Authorization Acts (NDAA). Key regulations include DFARS 225.7018, “Restriction on acquisition of certain magnets, tantalum, and tungsten,” and the corresponding contract clause, DFARS 252.225-7052.

These regulations prohibit the DoD from acquiring “covered materials” that originate from specific “covered countries”. The list of covered countries includes the People's Republic of China, the Russian Federation, the Democratic People's Republic of North Korea, and the Islamic Republic of Iran.

The scope of “covered materials” is explicitly defined to include:

- Samarium-cobalt (SmCo) magnets

- Neodymium-iron-boron (NdFeB) magnets

- Tantalum metals and alloys

- Tungsten metal powder

- Tungsten heavy alloy, including any finished or semi-finished components containing it

This framework is a direct response to national security concerns regarding supply chain vulnerabilities, particularly the concentration of rare earth mining and processing in China.

### Current Requirements and the 2027 Expanded Prohibition

The DFARS restrictions are being implemented in a phased approach, with a significant expansion of scope scheduled for January 1, 2027.

Current Rules (Effective through December 31, 2026): Through the end of 2026, the prohibition focuses on the final stages of metal and magnet production. Contractors are barred from delivering covered materials that were “melted or produced” in a covered country. For magnets, this specifically includes the melting of constituent elements to form the alloy (e.g., samarium with cobalt) and all subsequent manufacturing steps such as powder formation, pressing, sintering, and magnetization.

Expanded Prohibition (Effective January 1, 2027): A major shift occurs on January 1, 2027, when the prohibition expands to cover the entire upstream supply chain. From this date, contractors may not deliver any covered material that was “mined, refined, separated, melted, or produced” in a covered country. This change means that even if all magnet manufacturing steps occur in a compliant country, the use of rare earth oxides or metals that were mined or refined in a covered country will render the final product non-compliant. For SmCo and NdFeB magnets, this restriction explicitly includes the entire supply chain from the mining of ore or feedstock through the production of the finished magnet.

New legislative mandates also require enhanced transparency. The FY2023 NDAA requires contractors to disclose the provenance of permanent magnets containing rare earths, and if unable to do so, they must establish a supply chain tracking system. DOD is developing a corresponding DFARS rule, with a proposed version expected in late 2024.

### Nonavailability Determination Procedures

The DFARS provides a waiver mechanism for instances where compliant materials are not available. This process, detailed in DFARS 225.7018-4, allows for “nonavailability determinations,” which can be issued on an individual or class basis.

- Individual Determinations: These apply to a single contract and are authorized by the head of the contracting activity. The request must include supporting documentation and a written certification from the requiring activity that explains with specificity why alternatives are unacceptable. Templates and procedural guidance are available in the PGI.

- Class Determinations: These apply to more than one contract and require the approval of the Under Secretary of Defense for Acquisition and Sustainment (USD(A&S)). Before issuing a class determination, the USD(A&S) must publish a notice of intent on SAM.gov at least 30 days prior, soliciting information from interested parties on the availability of compliant materials.

In all cases, the nonavailability determination can be made if compliant materials of satisfactory quality and quantity, in the required form, cannot be procured as needed at a reasonable price.

### Recycled NdFeB Feedstock as a Compliant Pathway

The DFARS framework provides a specific and significant exception for recycled materials, creating a viable compliance pathway for NdFeB magnets. A neodymium-iron-boron magnet manufactured from recycled material is exempt from the sourcing restrictions, provided that both the milling of the recycled material and the sintering of the final magnet take place in the United States.

This statutory exception is a key enabler for the emerging domestic rare earth recycling industry. Companies are leveraging this provision to create DFARS-compliant feedstock for the defense industrial base.

Several companies are actively pursuing this pathway:

- Noveon Magnetics (formerly Urban Mining Company): Explicitly markets its NdFeB magnets, produced from recycled feedstock at its Texas facility, as DFARS-compliant. The company's patented Magnet-to-Magnet (M2M) process reuses end-of-life magnets, bypassing the mining and refining steps that are often tied to non-compliant sources.

- Cyclic Materials: This company is scaling up its capacity to produce recycled mixed rare earth oxides (rMREO) and has established a partnership with magnet manufacturer Vacuumschmelze (VAC) to recycle 100% of the manufacturing scrap from VAC's new U.S. facility. This creates a closed-loop, domestic source of feedstock.

- HyProMag USA: This venture is developing a facility to produce DFARS-compliant recycled NdFeB magnets using a hydrogen-based recycling process, with plans to begin full operations by 2027.

- ReElement Technologies: This company processes recycled magnets and provides traceability tokens to support contractor compliance, positioning its refined oxides as a domestic feedstock solution.

The broader Buy American Act framework further supports this, as one of its implementing regulations considers scrap that is “generated, collected, and prepared for processing in the United States” to be domestic material.

### Domestic Production Capacity Development

To address the systemic reliance on foreign sources, the DoD has launched a major initiative to reestablish a domestic “mine-to-magnet” supply chain. Since 2020, DoD has invested over $439 million through programs like the Manufacturing Capability Expansion and Investment Prioritization (MCEIP) directorate to fund every critical stage of the supply chain, from sourcing and separation to metallization, alloying, and magnet manufacturing. The stated goal is to create a sustainable supply chain capable of supporting all U.S. defense requirements by 2027.

Key vendors and investments include:

- MP Materials: As the operator of the only active rare earth mine in the U.S. at Mountain Pass, California, MP Materials has received significant DoD support, including a $400 million equity investment and a $150 million loan. This funding supports the expansion of its Texas magnetics facility and the construction of a new 10,000-metric-ton-per-year plant, with DoD committing to a 10-year offtake agreement and a price floor for NdPr products.

- Lynas USA, LLC: Awarded a combined $288 million to establish a second domestic, commercial-scale rare earth oxide production facility by 2026.

- Noveon Magnetics: Received over $35 million in DoD awards to support the commercialization of its recycled magnet production facility in Texas, which has a stated capacity of 2,000 metric tons per year.

- E-VAC Magnetics (a subsidiary of VAC): Awarded $94.1 million to establish a commercial-scale rare earth magnet manufacturing plant, expected to be completed by 2025.

These investments are intended to create a fully domestic ecosystem, ensuring that every critical node—from mining ore to producing finished magnets—can occur within the United States.

### GAO Audit Findings and Compliance Gaps

The Government Accountability Office (GAO) has repeatedly highlighted significant risks in the DoD's rare earth supply chain and identified gaps in its compliance and mitigation efforts. A central finding is the high potential for harm to national security stemming from overreliance on foreign sources, particularly China, for mining and processing.

Key compliance gaps identified by GAO include:

- Lack of Implementation: As of 2024, the DoD had not yet established clear policies or guidance to implement the statutory restriction on selling materials from the National Defense Stockpile to adversary nations.

- Limited Visibility: The DoD has limited insight into buyers' affiliations with adversary nations, often relying on “buyer self-attestation” for location and end-use information, a significant compliance vulnerability.

- Fragmented Approach: Past GAO reports found that the DoD's approach to identifying and mitigating risks was fragmented across different offices and that the department lacked the data to model its own requirements for over 40% of its designated strategic materials.

In response, the GAO has recommended that the DoD establish policies to prevent prohibited sales from the stockpile and enhance its methods for verifying buyer information. The DoD is also in the process of developing a new DFARS rule that will require contractors to disclose the provenance of permanent magnets, a direct response to legislative mandates aimed at improving supply chain transparency.

### Supplier Compliance Strategies

In response to the shifting regulatory landscape, key magnet suppliers to the defense sector are adopting various compliance strategies.

- Securing Compliant International Feedstock: Some suppliers are establishing supply chains that source raw materials and semi-finished magnet blocks from allied or neutral countries. Arnold Magnetic Technologies, for instance, established a supply chain with a German NdFeB supplier to provide blocks for final machining and finishing in the United States. Similarly, a consortium including Electron Energy Corporation (EEC) and Dexter Magnetic Technologies announced they are actively working with compliant global suppliers outside of China.

- Domestic Vertical Integration: The most robust strategy involves creating a fully domestic supply chain. The partnership between MP Materials and the DoD is the prime example, aiming for a complete “mine-to-magnet” ecosystem within the U.S..

- Leveraging Recycled Feedstock: As a direct pathway to DFARS compliance, companies are heavily investing in recycling. Noveon Magnetics bases its entire business model on producing DFARS-compliant magnets from recycled feedstock in its Texas facility. The partnership between Vacuumschmelze (VAC) and Cyclic Materials to recycle all of VAC's manufacturing scrap from its new South Carolina plant is another key example, creating a closed-loop system for a major new domestic producer.

- Proactive Compliance and Certification: Companies are proactively working towards the 2027 deadline. Arnold Magnetic Technologies states it is already fully compliant for its SmCo magnet applications. The EEC-led group is targeting mid-2026 for full DFARS 252.225-7052 compliance across its portfolio.

### Implications and Recommendations

The transition to a fully DFARS-compliant rare earth magnet supply chain by 2027 presents significant risks and opportunities for the defense industrial base. Defense prime contractors face the risk of supply disruptions and non-compliance if their subcontractors fail to secure compliant magnet sources. A proactive approach to supply chain management is essential, and contractors should already be engaging with their magnet suppliers to verify sourcing and map their transition plans for the 2027 deadline.

The role of recycled magnets is paramount in closing the compliance gap. The explicit DFARS exception for NdFeB magnets milled and sintered in the U.S. from recycled feedstock provides the most direct and near-term pathway for establishing compliant domestic production without reliance on foreign mining operations. This creates a clear market opportunity for companies specializing in rare earth recovery from scrap and end-of-life products.

For a wastewater treatment technology provider, this industrial shift presents several opportunities. The re-shoring of rare earth refining and recycling, particularly through hydrometallurgical processes, will generate new and complex industrial wastewater streams. These streams will contain dissolved rare earth elements, various acids, and other chemical reagents used in the leaching and separation processes. Technology providers who can offer efficient and cost-effective solutions for treating this wastewater—potentially including the recovery of valuable rare earth elements from the waste stream itself—will be well-positioned to serve this growing domestic industry.

Finally, the nonavailability determination process will likely be a critical tool during the transition period. Contractors and suppliers facing unavoidable gaps in compliant sourcing should begin aggregating the necessary data on market availability, technical requirements, and cost to support potential waiver requests through the procedures outlined in DFARS 225.7018-4.